## Slide 1: IDSS Docking Seal Interface Design
Preliminary Design Review (PDR)
IDSS Seal Design Team
2016-09-15

## Slide 2: Design Requirements
Seal must maintain cabin pressure across docking interface
Operating temperature: -100°C to +100°C
Design life: 10 docking cycles minimum
Leak rate: < 1.0 x 10^-4 scc/sec He at 14.7 psia

## Slide 3: Seal Configuration
Dual-seal configuration with inter-seal pressure monitoring
Primary seal: silicone elastomer (Esterline ELA-SA-401)
Secondary seal: fluorosilicone backup
Seal groove geometry: dovetail cross-section

## Slide 4: Interface Geometry
Seal diameter: 1524mm (60 inches)
Seal cross-section: 12mm x 8mm
Groove depth: 6.5mm
Compression: 25% nominal

## Slide 5: Open Items
TBD-SEAL-001: Final elastomer compound selection
TBD-SEAL-002: Seal compression range verification
TBD-SEAL-003: Low-temperature performance data
TBD-SEAL-004: Radiation degradation assessment

## Slide 6: Schedule
PDR: Complete
Material qualification: Q3 2017
Seal prototype test: Q4 2017
CDR: Q1 2018

## Slide 7: Summary & Next Steps
Questions?