## Slide 1: IDSS Docking Seal Interface Design
Critical Design Review (CDR)
IDSS Seal Design Team
2018-02-20

## Slide 2: Design Requirements (unchanged)
Seal must maintain cabin pressure across docking interface
Operating temperature: -100°C to +100°C
Design life: 10 docking cycles minimum
Leak rate: < 1.0 x 10^-4 scc/sec He at 14.7 psia

## Slide 3: Seal Configuration (final)
Dual-seal configuration with inter-seal pressure monitoring
Primary seal: Esterline ELA-SA-401 (qualified)
Secondary seal: Parker S0383-70 fluorosilicone
Seal groove geometry: dovetail, 15° sidewall angle
Retention: mechanical capture ring

## Slide 4: Qualification Test Results
Thermal cycling: 50 cycles, -100°C to +100°C — PASS
Compression set: 18% after 1000 hours at 100°C — PASS (req: <25%)
Leak rate at -50°C: 3.2 x 10^-5 scc/sec — PASS
Leak rate at +100°C: 7.8 x 10^-5 scc/sec — PASS
Docking cycle test: 15 cycles completed, no degradation

## Slide 5: Resolved TBDs
TBD-SEAL-001: RESOLVED — ELA-SA-401 selected and qualified
TBD-SEAL-002: RESOLVED — compression range 20-30% verified
TBD-SEAL-003: RESOLVED — leak rate meets spec to -80°C
TBD-SEAL-004: OPEN — radiation test scheduled Q2 2018

## Slide 6: Remaining Risk
Radiation degradation data pending (TBD-SEAL-004)
Mitigation: secondary seal provides redundancy
Long-term on-orbit compression set unknown
Mitigation: seal replacement capability designed in

## Slide 7: Summary & Next Steps
Questions?