## Slide 1: IDSS Docking Seal Interface Design
Flight Readiness Review (FRR)
IDSS Seal Design Team
2019-11-10

## Slide 2: Design Status: FLIGHT READY
All requirements verified by test
All TBDs resolved
Flight seals manufactured and inspected
Acceptance test complete
Ship review passed

## Slide 3: Final Qualification Summary
Thermal cycling: 100 cycles completed (2x requirement)
Compression set: 16% final (below 25% limit)
Leak rate worst case: 8.1 x 10^-5 at +100°C (below 1.0 x 10^-4 limit)
Docking cycle: 20 cycles (2x requirement)
Radiation: 25 krad total dose, no measurable degradation
All margins positive

## Slide 4: All TBDs Resolved
TBD-SEAL-001: CLOSED — ELA-SA-401 (PDR resolution)
TBD-SEAL-002: CLOSED — 20-30% compression verified (PDR)
TBD-SEAL-003: CLOSED — meets spec to -80°C (CDR)
TBD-SEAL-004: CLOSED — 25 krad no degradation (this review)

## Slide 5: Flight Unit Status
Lot acceptance test: PASS
Dimensional inspection: all within tolerance
Surface finish: Ra 0.4 (requirement Ra 0.8)
Shelf life: 5 years from cure date (manufactured 2019-03)
Installation window: 2020-2024

## Slide 6: Lessons Learned
Dovetail groove requires precision machining (±0.05mm)
Seal installation tool critical for consistent compression
Inter-seal monitoring provides real-time health indication
Second source qualification recommended for production

## Slide 7: Summary & Next Steps
Questions?